What is glass?

Glass is an amorphous (non-crystalline) solid material that exhibits a glass transition, which is the reversible transition in amorphous materials (or in amorphous regions within semicrystalline materials) from a hard and relatively brittle state into a molten or rubber-like state. Glasses are typically brittle and can be optically transparent.

What are alternative to Silica based glass?

metallic alloys, ionic melts, aqueous solutions, molecular liquids, and polymers. For many applications (bottles, eyewear) polymer glasses (acrylic glass, polycarbonate, polyethylene terephthalate)

Silica Glass

- Fused silica glass, vitreous silica glass: silica (SiO2). Has very low thermal expansion, is very hard and resists high temperatures (1000–1500 °C). It is also the most resistant against weathering (alkali ions leaching out of the glass, while staining it). It is used for high temperature applications such as furnace tubes, melting crucibles, etc.

- Soda-lime-silica glass, window glass: silica 72% + sodium oxide (Na2O) 14.2% + magnesia (MgO) 2.5% + lime (CaO) 10.0% + alumina (Al2O3) 0.6%. Is transparent, easily formed and most suitable for window glass. It has a high thermal expansion and poor resistance to heat (500–600 °C). Used for windows, containers, light bulbs, tableware.

- Sodium borosilicate glass, Pyrex: silica 81% + boric oxide (B2O3) 12% + soda (Na2O) 4.5% + alumina (Al2O3) 2.0%. Stands heat expansion much better than window glass. Used for chemical glassware, cooking glass, car head lamps, etc. Borosilicate glasses (e.g. Pyrex) have as main constituents silica and boron oxide. They have fairly low coefficients of thermal expansion (7740 Pyrex CTE is 3.25×10–6/°C  as compared to about 9×10−6/°C for a typical soda-lime glass[5]), making them more dimensionally stable. The lower CTE also makes them less subject to stress caused by thermal expansion, thus less vulnerable to cracking from thermal shock. They are commonly used for reagent bottles, optical components and household cookware.

- Lead-oxide glass, crystal glass: silica 59% + soda (Na2O) 2.0% + lead oxide (PbO) 25% + potassium oxide (K2O) 12% + alumina 0.4% + zinc oxide (ZnO) 1.5%. Has a high refractive index, making the look of glassware more brilliant (crystal glass). It also has a high elasticity, making glassware 'ring'. It is also more workable in the factory, but cannot stand heating very well.

- Aluminosilicate glass: silica 57% + alumina 16% + boric oxide (B2O3) 4.0% + barium oxide (BaO) 6.0% + magnesia 7.0% + lime 10%. Extensively used for fiberglass, used for making glass-reinforced plastics (boats, fishing rods, etc.). Also for halogen bulb glass.

- Oxide glass: alumina 90% + germanium oxide (GeO2) 10%. Extremely clear glass, used for fiber-optic wave guides in communication networks. Light loses only 5% of its intensity through 1 km of glass fiber.