## Slide 1: Chemistry 281(01) Winter 2017
Instructor: Dr. Upali Siriwardane
e-mail: upali@latech.edu
Office: CTH 311 Phone 257-4941

## Slide 2: Chapter 3. Structures of simple solids
Crystalline solids: The atoms, molecules or ions pack together in an ordered arrangement
Amorphous solids: No ordered structure to the particles of the solid. No well defined faces, angles or shapes
Polymeric Solids: Mostly amorphous but some have local crystiallnity. Examples would include glass and rubber.

## Slide 3: The Fundamental types of Crystals
Metallic: metal cations held together by a sea of electrons
Ionic: cations and anions held together by predominantly electrostatic attractions
Network: atoms bonded together covalently throughout the solid (also known as covalent crystal or covalent network).
Covalent or Molecular: collections of individual molecules; each lattice point in the crystal is a molecule

## Slide 4: Metallic Structures
Metallic Bonding in the Solid State:
Metals the atoms have low electronegativities; therefore the electrons are delocalized over all the atoms.
We can think of the structure of a metal as an arrangement of positive atom cores in a sea of electrons. For a more detailed picture see "Conductivity of Solids".
Metallic: Metal cations held together by a sea of valence electrons

## Slide 5: Metal Atom Packing
Close packing
Loose packing

## Slide 6: Metal Atom Packing

## Slide 7: Metal Atom Close Packing

## Slide 8: Packing and Geometry
Close packing
ABC.ABC... cubic close-packed CCP
gives face centered cubic or FCC(74.05% packed)
AB.AB... or AC.AC... (these are equivalent). This is called hexagonal close-packing HCP
CCP
HCP

## Slide 9: Packing and Geometry
Loose packing
Simple cube SC
Body-centered cubic BCC

## Slide 10: Unit Cell Dimensions
The unit cell angles are defined as:
a, the angle formed by the b and c cell edges
b, the angle formed by the a and c cell edges g, the angle formed by the a and b cell edges
a,b,c is x,y,z in right handed cartesian coordinates
a g b a c b a

## Slide 11: Bravais Lattices & Seven Crystals Systems
In the 1840’s Bravais showed that there are only fourteen different space lattices.
Taking into account the geometrical properties of the basis there are 230 different repetitive patterns in which atomic elements can be arranged to form crystal structures.

## Slide 12: Fourteen Bravias Unit Cells

## Slide 13: Seven Crystal Systems

## Slide 14: Number of Atoms in the Cubic Unit Cell
  Coner- 1/8
  Edge- 1/4
  Body- 1
  Face-1/2
  FCC = 4 ( 8 coners, 6 faces)
  SC = 1 (8 coners)
  BCC = 2 (8 coners, 1 body)
  Face-1/2
  Coner- 1/8
  Edge - 1/4
  Body- 1

## Slide 15: Close Pack Unit Cells
CCP
HCP
  FCC = 4 ( 8 coners, 6 faces)

## Slide 16: Unit Cells from Loose Packing
Simple cube SC Body-centered cubic BCC
  SC = 1 (8 coners)
  BCC = 2 (8 coners, 1 body)

## Slide 17: Coordination Number
The number of nearest particles surrounding a particle in the crystal structure.
Simple Cube: a particle in the crystal has a coordination number of 6
Body Centerd Cube: a particle in the crystal has a coordination number of 8
Hexagonal Close Pack &Cubic Close Pack: a particle in the crystal has a coordination number of 12

## Slide 18: Holes in FCC Unit Cells
Tetrahedral Hole (8 holes)
Eight holes are inside a face centered cube.
Octahedral Hole (4 holes)
One hole in the middle and 12 holes along the edges ( contributing 1/4) of the face centered cube

## Slide 19: Holes in SC Unit Cells
Cubic Hole

## Slide 20: Octahedral Hole in FCC
Octahedral Hole

## Slide 21: Tetrahedral Hole in FCC
Tetrahedral Hole

## Slide 22: Structure of Metals
Crystal Lattices A crystal is a repeating array made out of metals. In describing this structure we must distinguish between the pattern of repetition (the lattice type) and what is repeated (the unit cell) described above.

## Slide 23: Polymorphism
Metals are capable of existing in more than one form at a time
Polymorphism is the property or ability of a metal to exist in two or more crystalline forms depending upon temperature and composition. Most metals and metal alloys exhibit this property.
Uranium is a good example of a metal that exhibits polymorphism.

## Slide 24: Alloys
Substitutional
Second metal replaces the metal atoms in the lattice
Interstitial
Second metal occupies interstitial space (holes) in the lattice

## Slide 25: Properties of Alloys
Alloying substances are usually metals or metalloids. The properties of an alloy differ from the properties of the pure metals or metalloids that make up the alloy and this difference is what creates the usefulness of alloys. By combining metals and metalloids, manufacturers can develop alloys that have the particular properties required for a given use.

## Slide 26: Structure of Ionic Solids
Crystal Lattices A crystal is a repeating array made out of ions. In describing this structure we must distinguish between the pattern of repetition (the lattice type) and what is repeated (the unit cell) described above.
Cations fit into the holes in the anionic lattice since anions are lager than cations.
In cases where cations are bigger than anions lattice is considered to be made up of cationic lattice with smaller anions filling the holes

## Slide 27: Basic Ionic Crystal Unit Cells

## Slide 28: Radius Ratio Rules
r+/r- Coordination Holes in Which
Ratio Number Positive Ions Pack
0.225 - 0.414 4 tetrahedral holes FCC
0.414 - 0.732 6 octahedral holes FCC
0.732 - 1 8 cubic holes BCC

## Slide 29: Cesium Chloride Structure (CsCl)

## Slide 30: Rock Salt (NaCl)
© 1995 by the Division of Chemical Education, Inc., American Chemical Society.
Reproduced with permission from Soli-State Resources.

## Slide 31: Sodium Chloride Lattice (NaCl)

## Slide 32: NaCl Lattice Calculations

## Slide 33: CaF2

## Slide 34: Calcium Fluoride
© 1995 by the Division of Chemical Education, Inc., American Chemical Society.
Reproduced with permission from Solid-State Resources.

## Slide 35: Zinc Blende Structure (ZnS)

## Slide 36: Lead Sulfide
© 1995 by the Division of Chemical Education, Inc., American Chemical Society.
Reproduced with permission from Solid-State Resources.

## Slide 37: Wurtzite Structure (ZnS)

## Slide 38: Packing Efficiency

## Slide 39: Packing Efficiency

## Slide 40: Summary of Unit Cells
Volume of a sphere = 4/3pr3
Volume of sphere in SC = 4/3p(½)3 = 0.52
Volume of sphere in BCC = 4/3p((3)½/4)3 = 0.34
Volume of sphere in FCC = 4/3p( 1/(2(2)½))3 = 0.185

## Slide 41: Density Calculations
Aluminum has a ccp (fcc) arrangement of atoms. The radius of Al = 1.423Å ( = 143.2pm). Calculate the lattice parameter of the unit cell and the density of solid Al (atomic weight = 26.98).
Solution:
4 atoms/cell [8 at corners (each 1/8), 6 in faces (each 1/2)]
Lattice parameter: a/r(Al) = 2(2)1/2
a = 2(2)1/2 (1.432Å) = 4.050Å= 4.050 x 10-8 cm
Density = 2.698 g/cm3

## Slide 42: Lattice Energy
The Lattice energy, U, is the amount of energy required to separate a mole of the solid (s) into a
gas (g) of its ions.

## Slide 43: Lattice energy
The higher the lattice energy, the stronger the attraction between ions.
Lattice energy
Compound kJ/mol
LiCl 834
NaCl 769
KCl 701
NaBr 732
Na2O 2481
Na2S 2192
MgCl2 2326
MgO 3795

## Slide 44: Lattice Energy

## Slide 45: Properties of Ionic Compounds
Crystals of Ionic Compounds are hard and brittle
Have high melting points
When heated to molten state they conduct electricity
When dissolved in water conducts electricity

## Slide 46: Trends in Melting Points
Compound Lattice Energy
(kcal/mol)
NaF -201
NaCl -182
NaBr -173
NaI -159

## Slide 47: Trends in Melting Points
Compound Lattice Energy
(kcal/mol)
NaF -201
NaCl -182
NaBr -173
NaI -159

## Slide 48: Trends in Properties
Compound q+ radius q- radius M.P (oC) L.E. (kJ/mol)
LiCl 0.68 1.81 605 834
NaCl 0.98 1.81 801 769
KCl 1.33 1.81 770 701
LiF 0.68 1.33 845 1024
NaF 0.98 1.33 993 911
KF 1.33 1.33 858 815
MgCl2 0.65 1.81 714 2326
CaCl2 0.94 1.81 782 2223
MgO 0.65 1.45 2852 3938
CaO 0.94 1.45 2614 3414

## Slide 49: Coulomb’s Law
k = constant
q+ = cation charge
q- = anion charge
r = distance between two ions

## Slide 50: Coulomb’s Model
where e = charge on an electron = 1.602 x 10-19 C
e0 = permittivity of vacuum = 8.854 x 10-12 C2J-1m-1
ZA = charge on ion A
ZB = charge on ion B
d = separation of ion centers

## Slide 51: Ionic Bonds
An ionic bond is simply the electrostatic attraction between opposite charges.
Ions with charges Q1 and Q2:
The potential energy is given by:
d
·
·
d
Q
Q
E
2
1
µ

## Slide 52: Estimating Lattice Energy
Arrange with increasing lattice energy:
KCl
NaF
MgO
KBr
NaCl
788 kJ
671 kJ
3795 kJ
910 kJ
701 kJ
d
·
·
K+
Cl
·
·
K+
Br
d
d
Q
Q
E
2
1
µ

## Slide 53: Madelung Constant
Madelung constant is geometric factor that depends on the lattice structure.

## Slide 54: Madelung Constant Calculation

## Slide 55: Degree of Covalent Character
Fajan's Rules (Polarization)Polarization will be increased by:
  1. High charge and small size of the cation
  2. High charge and large size of the anion
  3. An incomplete valence shell electron configuration

## Slide 56: Trends in Melting Points Silver Halides
Compound M.P. oC
AgF 435
AgCl 455
AgBr 430
AgI 553

## Slide 57: Born-Lande Model:
This modes include repulsions due to overlap of electron electron clouds of ions.
eo = permitivity of free space
A = Madelung Constant
ro = sum of the ionic radii
n = average born exponet depend on the electron configuration

## Slide 58: Born_Haber Cycle
Energy Considerations in Ionic Structures

## Slide 59: Born-Haber Cycle?
Relates lattice energy ( L.E) to:
Sublimation (vaporization) energy (S.E)
Ionization energy metal (I.E)
Bond Dissociation of nonmetal (B.E)
DHf formation of NaCl(s)
L.E. = E.A.+ 1/2 B.E. + I.E. + S.E. - DHf

## Slide 60: Ionic bond formation

## Slide 61: Energy and ionic bond formation
Example - formation of sodium chloride.
Steps DHo, kJ
Vaporization of Na(s) Na(g) +92
sodium
Decomposition of 1/2 Cl2 (g) Cl(g) +121
chlorine molecules
Ionization of sodium Na(g) Na+(g) +496
Addition of electron Cl(g) + e- Cl-(g) -349
to chlorine
( electron affinity)
Formation of NaCl Na+(g)+Cl-(g) NaCl -771

## Slide 62: Energy and ionic bond formation
Na(s) + 1/2 Cl2(g)
Na(g) + 1/2 Cl2(g)
Na(g) + Cl(g)
Na+(s) + Cl(g)
Na+(s) + Cl-(g)
NaCl(s)
+496 kJ(I.E.)
+121 kJ(1/2 B.D.E.)
+92 kJ(S.E.)
-349 kJ (E.A.)
-771 kJ (L.E.)
-411 kJ(DHf)

## Slide 63: Calculation of DHf from lattice Energy

## Slide 64: Hydration of Cations

## Slide 65: Solubility: Lattice Energy and Hydration Energy
Solubility depends on the difference between lattice energy and hydration energy holds ions and water.
For dissolution to occur the lattice energy must be overcome by hydration energy.

## Slide 66: Solubility: Lattice Energy and Hydration Energy
For strong electrolytes lattice energy increases with increase in ionic charge and
decrease in ionic size
H hydration energies are greatest for small, highly charged ions
Difficult to predict solubility from size and charge of ions. we use solubility rules.

## Slide 67: Thermodynamics of the Solution Process of Ionic Compounds
Heat of solution, DHsolution :
Enthalpy of hydration, DHhyd,
Lattice Energy, Ulatt

## Slide 68: Solution Process of Ionic Compounds

## Slide 69: Enthalpy from dipole – dipole Interactions
The last term, DH L-L, indicates the loss of enthalpy from dipole - dipole interactions between solvent molecules (L) when they become solvating ligands (L') for the ions.

## Slide 70: Hydration Process

## Slide 71: Different types of Interactions for Dissolution

## Slide 72: Hydration Energy of Ions

## Slide 73: Hydration Process

## Slide 74: Calculation of DHsolution

## Slide 75: Heat of Solution and Solubility

## Slide 76: Metallic Bonding Models
The difference in chemical properties between metals and non-metals lie mainly in the fact those atoms of metals fewer valence electrons and they are shared among all the atoms in the substance: metallic bonding.

## Slide 77: Metallic solids
Repeating units are made up of metal atoms,
Valence electrons are free to jump from one atom to another
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+

## Slide 78: Electron-sea model of bonding
The metallic bond consists of a series of metals atoms that have all donated their valence electrons to an electron cloud, referred to as an electron sea which permeates the entire solid. It is like a box (solid) of marbles (positively charged metal cores: known as Kernels) that are surrounded by water (valence electrons).

## Slide 79: Electron-sea model Explanation
Metallic bond together is the attraction between the positive kernels and the delocalized negative electron cloud.
Fluid electrons that can carry a charge and kinetic energy flow easily through the solid making metals good electrical and thermal conductor.
The kernels can be pushed anywhere within the solid and the electrons will follow them, giving metals flexibility: malleability and ductility.

## Slide 80: Delocalized Metallic Bonding
Metals are held together by delocalized bonds formed from the atomic orbitals of all the atoms in the lattice.
The idea that the molecular orbitals of the band of energy levels are spread or delocalized over the atoms of the piece of metal accounts for bonding in metallic solids.

## Slide 81: Molecular orbital theory
Molecular Orbital Theory applied to metallic bonding is known as Band Theory.
Band theory uses the LCAO of all valence atomic orbitals of metals in the solid to form bands of s, p, d, f bands (molecular orbitals) just like simple molecular orbital theory is applied to a diatomic molecule, hydrogen(H2).

## Slide 82: Types of conducting materials
a) Conductor (which is usually a metal) is a solid with a partially full band.
b) Insulator is a solid with a full band and a large band gap.
c) Semiconductor is a solid with a full band and a small band gap.

## Slide 83: Linear Combination of Atomic Orbitals

## Slide 84: Linear Combination of Atomic Orbitals

## Slide 85: Conduction Bands in Metals

## Slide 86: Types of Materials
A conductor (which is usually a metal) is a solid with a partially full band
An insulator is a solid with a full band and a large band gap
A semiconductor is a solid with a full band and a small band gap
Element Band Gap C 5.47 eV Si 1.12 eV Ge 0.66 eV Sn 0 eV

## Slide 87: Band Gaps

## Slide 88: Band Theory of Metals

## Slide 89: Band Theory
Insulators – valence electrons are tightly bound to (or shared with) the individual atoms – strongest ionic (partially covalent) bonding.
Semiconductors - mostly covalent bonding somewhat weaker bonding.
Metals – valence electrons form an “electron gas” that are not bound to any particular ion

## Slide 90: Bonding Models for Metals
Band Theory of Bonding in Solids
Bonding in solids such as metals, insulators and semiconductors may be understood most effectively by an expansion of simple MO theory to assemblages of scores of atoms

## Slide 91: Band Gaps

## Slide 92: Doping Semiconductors